**Division 07 2100 • Division 09 8000**

**Spray Applied Thermal and Acoustic Solutions**

(Total = 3 pages)

**PART 1 GENERAL**

* 1. **Related Works and Sections**
		1. Division 07 2100 - Building Insulation

Division 09 8000 - Acoustic insulation

* 1. **Work Included**
		1. Provide all materials, labour, equipment and services necessary for, and incidental to, the complete and correct installation of all TC-417 and related work as shown on the drawings or where specified herein, and in accordance with all applicable requirements of the Contract documents.
		2. All material and installation shall conform to the applicable and/or other code requirements of all authorities having jurisdiction.

* 1. **Quality Assurance**
		1. If requested, provide samples of minimum size 90mm x 121mm (3.5" x 4.75”) of sprayed TC-417 on a rigid backing appropriate to the installation.
		2. Work shall be performed by a firm with a

minimum 3 years experience in the sprayed insulation and/or fireproofing business and shall possess expertise in the installation of TC-417 and shall be currently registered as an approved Applicator by ThermaCoustic Industries International Limited.

* + 1. Before proceeding with the application of TC-417 thermal and acoustic insulation, approval of the proposed material thickness shall be obtained from the architect and other applicable authorities.
	1. **Manufacturer's Literature**
		1. Copies of the manufacturer's literature, clearly indicating conditions of acceptance and method of application, shall be available on site before and during period of performance of related work and product installation.
	2. **Material Delivery and Storage**
		1. All material to be delivered to the site in original, undamaged and unopened packages clearly labelled as TC-417.
		2. All materials to be stored on site in a warm, dry location on either a concrete floor or raised platform. Material must **not** get damp or wet.
		3. TC-417 adhesive must **not** freeze.
	3. **Project Conditions**
		1. TC-417 shall only be installed under the conditions as stated in the manufacturer's published application instructions.
		2. When the prevailing outdoor temperature at the site is less than 4 0C (400  F), a minimum substrate and ambient temperature of 4 0C (400  F) shall be maintained for 24h before, during and until the applied product is completely cured (dry) through to the substrate. If necessary for job progress, the General Contractor shall provide enclosures with **dry** heat to maintain temperature.
		3. General Contractor shall provide ventilation to allow proper drying of the installed TC-417 during and after its application.
		4. At all times during installation and drying of TC-417 ventilation in enclosed areas shall not be less that 3 complete air changes per hour.
		5. For roof deck applications TC-417 must be completely dried and cured before any roof traffic or activities resume. The contractor shall confirm that the deflection of the roof deck is not greater then1/120 clear span.
		6. All patching and repairing of installed TC- 417 required because of damage or cutting by other trades shall be

performed under this Section and paid for by the trade(s) responsible.

* + 1. The General Contractor shall allow the Manufacturer's representative full access to the site during normal working hours.
		2. The Contractor shall co-operate in the co-ordination and scheduling of the insulation work to avoid delays in job progress.

**PART 2 PRODUCTS**

* + 1. Materials: spray-applied material shall be TC-417 white glass fibre together with TC-417 GP synthetic emulsion adhesive conforming to CAN 4-S114 and ASTM E-136 as manufactured by ThermaCoustic Industries International Limited.
		2. Spray applied material shall be TC-417 white glass fibre conforming to CAN 4-S114-78 using TC-417 GP adhesive manufactured by ThermaCoustic Industries International Limited.

* + 1. TC-417 shall not contain free crystalline silica, asbestos or combustible fibre, and shall exhibit the following qualities according to the test protocols quoted:

ASTM C-518: R = 4.17/in; RSI = 29.32/m

 K = 0.24; λ = 0.0346

CAN/ULC S-114: Non-combustible

ASTM E-136: Non-combustible

CAN/ULC S-102:

ASTM E-84: Flame spread = < 25;

 Smoke development = < 50

ASTM C-423 90a: NRC = 1.00 (50mm/2 in.)

ISO 354: NRC = 0.95 (50mm/2 in.)

* + 1. ThermaCoustic Industries TC-417 Adhesive shall be mixed with fresh, clean, potable water in the exact proportion as recommended by the manufacturer.
		2. TC-417 adhesive **must be kept**

**from freezing at all times**.

**PART 3 EXECUTION**

**3.1 Preparation**

* + 1. All surfaces to receive TC-417 spray Insulation shall be free of all petroleum-based greases and oils, loose mill scale, rust, poorly adhered paint and other foreign materials that could impair bonding to the surface. Any required cleaning of the substrate to receive TC-417 shall be the responsibility of the General Contractor.
		2. Remove dust, dirt or foreign material on surfaces to which the product is to be applied, that could otherwise create a false bond or surface staining of the product.
		3. Verify compatibility and bond requirements of all

surfaces to receive TC-417.

* + 1. Ensure that all equipment, piping, ducts or other units that would interfere with the application of TC-417 are not positioned until application is complete.
		2. Ensure that proper temperature and ventilation are maintained as specified in 1.6.2 through 1.6.4.
		3. Provide and install masking, drop cloths or other suitable coverings to prevent overspray from

coming into contact with unintended fixtures and surfaces.

* 1. **Application**
		1. Mix and apply TC-417 in strict accordance with manufacturer's published recommendations.
		2. Apply product in sufficient thickness to achieve the required thermal and/or acoustic value.
		3. Use a 'one-pass' application procedure. Do **not**

 layer application.

* 1. **Clean-up**
		1. Remove overspray from equipment and surfaces not intended to be covered. Perform all removal work while installed product is still wet.

* + 1. Ensure clean up is up to industry standards.
	1. **Options**
		1. The surface of TC-417 can be left untamped for basic finish, or can be board tamped and oversprayed for a flatter, more uniform finish.
		2. For a more durable and attractive finish in exposed areas we recommend the surface be board tamped and oversprayed with TC-417 adhesive.
		3. If a finish colour other than white is desired we suggest:
1. For dark grey (charcoal) or light grey use our colour additives for TC-417 adhesive;
2. Otherwise, paint the installed TC-417 with any good quality emulsion paint of the desired colour.

© 2018 THERMACOUSTIC INDUSTRIES INT’L. LTD.